## Slide 1: دانشکده مهندسی مکانیک و انرژی مهندسی پودر
نیمسال اول 1405-1404
‏دوشنبه (10:30-9:00)

## Slide 2: فهرست مطالب
فهرست مراجع
شیوه ارزیابی
سرفصل دروس

## Slide 3: فهرست مراجع
An Introduction to Powder Metallurgy; F. THUMMLER and R.OBERACKER, © 1993 The Institute of Materials.
ASM Handbook; Volume 7, Powder Metal Technologies and Applications.
Presentation files related to each topics

## Slide 4: شیوه ارزیابی
میان‏ترم (6 تا 9 نمره ) + پایان ترم (9 تا 12)+ حضور فعال در کلاس (1 نمره اضافی)
تاریخ امتحان میان ترم: چهارشنبه 12 آذر 1404
انتخاب نماینده کلاس
امکان مراجعه حضوری جهت رفع اشکال: یکشنبه ها ساعت 12:30 الی 13:30

## Slide 5: سرفصل دروس

## Slide 6: An Introduction
Definition of Powder Metallurgy
Powder metallurgy may defined as, “the art and science of producing metal powders and utilizing them to make serviceable objects.”
OR
It may also be defined as “material processing technique used to consolidate particulate matter i.e. powders both metal and/or non-metals.”
OR
is a process whereby a solid metal, alloy or ceramic in the form of a mass of dry particles is converted into an engineering component of predetermined shape and possessing properties which allow it to be used in most cases without further processing.

## Slide 7: An Introduction
Powder metallurgy is a forming and fabrication technique consisting of three major processing stages.
– First, the primary material is physically powdered, divided into many small individual particles.
– Next, the powder is injected into a mold or passed through a die to produce a weakly cohesive structure (via cold welding) very near the dimensions of the object ultimately to be manufactured.
– Finally, the end part is formed by applying pressure,

## Slide 8: An Introduction

## Slide 9: An Introduction
Metal processing technology in which parts are produced from metallic powders.
PM parts can be mass produced to net shape or near net shape, eliminating or reducing the need for subsequent machining.
PM process wastes very little material ~ 97% of starting powders are converted to product.
PM parts can be made with a specified level of porosity, to produce porous metal parts.
Examples: filters, oil-impregnated bearings and gears.
Certain metals that are difficult to fabricate by other methods can be shaped by PM.

## Slide 10: An Introduction
PM vs. Other Fabrication Methods (casting, stamping or machining)
• PM is the choice when requirements for strength, wear resistance or high operating temperatures exceed the capabilities of die casting alloys.
• PM offers greater precision, eliminating most or all of the finish machining operations required for castings.
• It avoids casting defects such as blow holes, shrinkage and inclusions. Powder injection molding is coming out as a big challenge for investment casting.
• However the PM process is economical only when production rates are higher, since the tooling cost is quite appreciable.

## Slide 11: An Introduction
The powder Metallurgy methods starts with powders and the properties of the manufactured parts depend to a large extent on the properties of the initial powders. Amongst powder properties, composition, size, form and structure of particle, specific surface, porosity and volume characteristics, fluidity, strength, hardness, permeability regarding liquids and gases, electric conductivity, compressibility and sinterability are of great importance in powder metallurgy.
Metal powders consist of separate small bodies—the so- called particles—from 0.1 μ up to several millimeters in size.
In the majority of powders the size of particle varies from several microns to 0.5 mm. Particles usually have internal pores, cracks and impurities.

## Slide 12: An Introduction
Particle shape is widely varied and determined by the methods of production; the desired particle size is obtained by regulating the conditions of manufacture.
Particles are divided according to their shape into three basic groups:
(1 ) hair or needle-shaped, the lengths of which considerably exceed their other dimensions;
(2) flat (flakes or leaves) whose length and breadth are many times greater than their thickness;
(3) equiaxed, which are roughly identical in all dimensions.

## Slide 13: An Introduction
Powders of the same chemical composition, but with different physical characteristics, are sharply distinguished by technological properties, i.e. by their behaviour during processing.
Production methods and the fields of application for powders are determined with powder properties (shape, size)
Example: copper powder with particles in the form offtakes (flat) up to 1 μ thick and up to 50μ in diameter are used only as a pigment since any articles made from it contain cracks after pressing.
Copper powder with particles of spherical form (globules) from 100 to 700μ in diameter is pressed only at very high pressures.
A powder with irregularly shaped particles, so called dendritic, 40-45μ in size is easily pressed even at low pressures.

## Slide 14: An Introduction

## Slide 15: An Introduction

## Slide 16: An Introduction

## Slide 17: An Introduction

## Slide 18: An Introduction

## Slide 19: An Introduction

## Slide 20: An Introduction

## Slide 21: An Introduction

## Slide 22: An Introduction
The mid-1920s saw the emergence of two powder metallurgy products which set the patterns for the future industrial development of the technology. The first of these was a hard, wear-resisting product known as cemented carbide, which is produced by compacting and sintering a mixture of powders of tungsten carbide with up to 15% of cobalt. At a temperature of about 1400°C, a molten phase is formed between the cobalt and some of the tungsten carbide and this promotes rapid and virtually complete densification to give a final structure of carbide particles in a tungsten carbide/cobalt alloy matrix. Developed originally for wire-drawing dies, cemented carbides have found extensive application in metal cutting, rock drilling and hot working dies. Many new compositions have been developed including additions of other refractory metal carbides such as tantalum and titanium.
While tungsten carbide refers to the specific material combining tungsten and carbon, cemented carbide is actually a broader category that includes tungsten carbide bound with a metal binder (usually cobalt)

## Slide 23: An Introduction
The second significant development was the porous bronze self-lubricating bearing, which was invented in the late 1920s, and which is made from a mixture of 90% copper, 10%tin powders, usually with a small graphite addition. The powder mixture is pressed and sintered to form a tin-bronze alloy with little dimensional change, and containing up to 35% of fine, interconnected, porosity. The final close dimensional tolerances required in the bearing are achieved by pressing the sintered compact in a sizing die after which it is impregnated with oil. When in use, the bronze reservoir supplies oil to the bearing interface. Other porous products today include filters for separation processes made from lightly compacted and sintered powders of, for example, bronze or stainless steel.

## Slide 24: Powder Production Techniques
The most important metal powders are: iron and steel, copper and copper base, aluminium, nickel, molybdenum, tungsten, tungsten carbide and tin. Besides metallic powders also carbide, nitride, boride and special ceramic powders as well as whiskers and short fibers are considered.
MECHANICAL PROCESSES
The size reduction of metal powders by mechanical means is performed in the solid state as well as of melts. Grinding and milling are the oldest processes in powder metallurgy and ceramics for the production of particulate materials. They are extensively applied in the field of ceramics and in the cement industry for size reduction of brittle materials, often accompanied by intensive mixing effects.

## Slide 25: Powder Production Techniques
Their use in powder metallurgy is more limited, since the disintegration of metallic materials, which mostly exhibit considerable plasticity, is less effective. Nevertheless, materials such as intermetallic compounds and ferroalloys can be effectively comminuted by mechanical means. Additionally, there are important mechanical disintegration processes in powder metallurgy, especially those involving high energy milling procedures, during which severe embrittlement of the metal occurs. This aspect can be turned to advantage in the process known as mechanical alloying.
The general phenomena during size reduction in the solid state are based on fracture mechanics: the nucleation of cracks, followed by crack propagation and fracture, by which new surfaces are formed. A further decrease of mean particle size can take place only when these processes occur.

## Slide 26: Powder Production Techniques
The kinetic energy within the milling aggregate is partially transformed into mechanical stresses in the material to be disintegrated. The forces acting in these processes cause mainly compression and shear stresses, applied as impact or slow-acting stresses by the milling balls during vessel rotation or vibration, or by the rotating arms in an attritor. In plastic materials, gross dislocation formation and movement, i.e. plastic deformation, is induced before cracking and fracturing occur. In ceramic materials, plastic deformation does not take place in coarse particles, but becomes significant for mean particle sizes in the micron range. The main process phenomenon for all grinding and milling processes, however, is crack propagation and fracture, which is accompanied by local, not well defined, temperature rises. These are often referred to as thermal 'spikes' and can result in anomalous structures.

## Slide 27: Powder Production Techniques
The limit of the minimum obtainable particle size depends on the conditions of the mechanical process as well as on the material itself. This so-called grinding or milling equilibrium, has been investigated for many metallic and non-metallic powders. It ranges between roughly 0.1 and 1 micron and can be explained by several independent processes as follows:
• In a solid material there is no constant binding force within the volume but only a binding spectrum, dependent on the local types of defects and defect concentration. These can be macro, micro or on an atomic scale. Only the weaker part of the binding spectrum can be destroyed by mechanical means, and a further reduction in size of small particles becomes increasingly difficult.

## Slide 28: Powder Production Techniques
The smaller the particle size the more difficult is the application of the necessary shear stress on each particle in order to achieve further particle fracture. With small particles the elastic or elasto-plastic response to mechanical stresses becomes dominating. Small particles exhibit higher surface activity than larger ones and therefore, have a higher probability of being re-welded. This was previously believed to be the main reason for the 'milling equilibrium' observed.

## Slide 29: Powder Production Techniques
The efficiency of mechanical size-reduction processes is generally very low. Only about 0.1% of the spent energy in the conventional ball milling process is found in the generated new surfaces of the fine particles. The energy E necessary for the physical process of size reduction is given by
E=γ. ∆S
where γ = the specific surface energy and ∆S = the increase of specific surface. The efficiency may be somewhat higher in high energy milling processes, but is still less than 1%. The percentage figure becomes larger when, instead of the energy defined in equation (2.1), the energy necessary for crack propagation is considered - being about one order of magnitude larger.

## Slide 30: Powder Production Techniques
The sources of 'lost energy' are many: they include the elastic and plastic deformation of the particles, the kinetic energy of the particles in motion, impact and friction energy in the form of heat outside the powder, etc. The main cause of lost energy, however, is the generation of heat. In order to optimize milling efficiency special conditions have to be established.
• in conventional steel ball mills, defining the size and number of milling balls which will take up 40-50% of the vessel volume. The size of the balls generally ranges between 12 and 16 mm, about 10-20 times larger than the initial size of the particles to be milled.
using vibration milling instead of milling by vessel rotation. The impact intensity of the milling balls is much higher in vibration milling than in the 'falling' process in rotational ball milling. The noise level, however, of a vibration mill is very high. Such mills were used for a long time in the fabrication of cemented carbides, but have now mostly been replaced by attritors. For laboratory purposes discs are used successfully instead of balls in vibration milling.

## Slide 31: Powder Production Techniques
other types of fine-milling equipment, such as planetary ball milling, centrifugal milling and attritor milling are widely used.
• wet milling instead of dry milling is often advantageous because liquids tend to break up agglomerates as well as reducing re-welding of powder particles. As milling media, hydrocarbons (hexane, heptane), ethanol and other organic liquids, which help to avoid oxidation of the milled product, are often used. Special effects have been achieved by using surface active additives (e.g. oleinic acid or other substances with a long carbon chain and a surface active group), which reduce the interfacial energy between particles and the milling media (Rehbinder-Effect) and, more importantly, increase the crack propagation during milling by reducing the cohesion at crack tips.

## Slide 32: Powder Production Techniques
During the milling of hard and abrasive powders the level of impurities sometimes rises considerably, because of severe wear loss from walls and milling media. Iron contamination can be removed by subsequent acid leaching, when the milled powder itself is acid-resistant. Rubber liners and ceramic balls (Al203) which cause less contamination are sometimes advisable. The best but most expensive solution is to use liners and balls of similar composition to that of the material being milled (e.g., the milling of special ceramic powders, like Si3N4)·
Equipment
There is a wide variety of grinding and milling equipment, but the following are selected for particular mention:

## Slide 33: Powder Production Techniques
Ball and Vibration Milling
Figure 2.1 shows the principles of conventional steel ball mills, which are available from a small laboratory size (less than 1 litre) to very large sizes used mainly for the ceramic and cement industry. At too low rotation speed the milling balls are mainly rolling over each other, but at higher speed some of the balls are in free fall at each moment (Fig. 2.1), which is the optimum condition for the milling process. At too high speed, however, the centrifugal forces hinder the balls in free fall. Ball mills are sometimes used in powder metallurgy for mixing purposes only. In vibration mills the design of the vessel is similar to that in rotation ball mills, but the vessel is mounted on special steel springs. The amplitude as well as the frequency of vibration can be adjusted according to the characteristics of the vibrating mechanism and the springs. Vibration mills are often used with only short milling times in research and development for size reduction of inorganic and organic products.

## Slide 34: Powder Production Techniques
The difference from the conventional ball mill is the superposition of the single vessel rotation by
rotation of the table supporting the fixed vessels, which accelerates the movement of the
milling balls. Centrifugal accelerations up to 20 g (acceleration due to gravity) are possible.
Attritor milling
An attritor is a ball milling system in which the balls, together with the material to be milled are set in motion by a shaft with stirring arms, rotating at 100-300, small units up to 2000 rpm. The containing cylindrical vessel is usually water cooled because of the considerable heat generated by the process. The process may be undertaken dry, or wet with water or organic liquids. The balls are generally smaller (0.5-2 mm) than in conventional ball mills. For production scales the process can be run continuously by feeding the vessel from the bottom while unloading the milled product from the top. A closed cycle can be provided for the milling liquid, including distillation apparatus for recycling.

## Slide 35: Powder Production Techniques
For processing of materials with special oxidation sensitivity (e.g., powders for Co-rare-earth-magnets) the attritor can be equipped with an inert gas supply, which is generally advisable in dry milling.
A definite ratio of milling balls to milling material is essential for optimum efficiency. Figures 2.3 and 2.4 show two types of attritors. Discs with holes or profiled discs are also used instead of arms as rotating units in so called agitation ball mills. The milling intensity of an attritor is generally much higher than that of conventional ball mills, the difference being at least one order of magnitude in time for achieving similar results (see Fig. 2.5). In addition to compression stresses, high rate shear stresses are involved leading to lower energy losses compared with other processes.

## Slide 36: Powder Production Techniques

## Slide 37: Powder Production Techniques
Dry and wet attritors are widely employed for inorganic pigment and paint production, for limestone, and oxides, and in the hard-metal industry, where they have replaced vibration mills. In these fields of application very fine particulates are required. In the powder mixtures for cemented carbide manufacture (e.g. WC-Co), a certain degree of 'coating' of the brittle carbide by the ductile cobalt particles during milling-mixing occurs which is desirable for further processing. Several metals and alloys may become amorphous during extended milling in an attritor. Investigations, mainly during the last decade, have resulted in the development of tailor-made amorphous alloys (glassy metals), by this method.
Roller Milling
For brittle materials a new size reduction technology become important, the high-compression roller mill, Fig. 2.6, which operates with profiled rollers in the pressure range 50-500 MPa. According to the working conditions products with narrow particle size ranges, between 200 and about 5 micron are achievable. The service life is claimed to be 10 to 20 times that of ball mills.
A metal or alloy with high hardness

## Slide 38: Powder Production Techniques
The Cold Stream Process
In this process coarse particles (less than 2 mm) are transported in a high pressure, high-velocity gas stream and shot on to a target of a highly wear resistant material. A typical pressure of the system is 70 bar with a gas velocity up to Mach 1 or even higher. Due to the drop in pressure of the gas stream on passing through a venturi-nozzle before entering the collision chamber at lower than atmospheric pressure, a rapid cooling of the particles occurs in the nearly adiabatic system. This leads to considerable particle embrittlement and allows easy particle fracturing during collision with the target. The particle fines are extracted from the continuously repeated process and collected in special chambers, while the coarser fractions stay in the cycle. By using inert gas (Ar) the process provides fine powders (a few micron) with very low oxygen content. The surface oxides of the raw material can be spalled off and separated during the first few cycles. The cost of the process is high partly due to high energy consumption. This results in economic powder production only for materials with a high value, such as superalloys, cemented carbides, etc.

## Slide 39: Powder Production Techniques
در این سیستم، گاز با عبور از گلوگاه نازل ونتوری، سرعتش زیاد شده و فشارش افت می‌کند. از آنجایی که این فرآیند به صورت آدیاباتیک (بدون تبادل گرما با بیرون) رخ می‌دهد، انرژی درونی گاز کاهش یافته و دمای آن به شدت پایین می‌آید، که این سرمایش سریع به ذرات معلق نیز منتقل می‌شود. این اثر برای کنترل اندازه و ساختار نانوذرات بسیار مهم است.
افت فشار شدید در گلوگاه ونتوری باعث می‌شود که گاز با سرعت زیاد منبسط شود.
این فرآیند در محیطی با فشار کمتر از فشار اتمسفر (خلاء نسبی) رخ می‌دهد که این شرایط انبساط را تشدید می‌کند.
کاهش ناگهانی فشار گاز (انبساط آدیاباتیک) باعث می‌شود که انرژی درونی گاز صرف کار انبساط شود. این اتلاف انرژی باعث می‌شود دمای گاز به شدت افت کند.
ذرات معلق در این جریان گازی، به سرعت دمای خود را با دمای گاز میزبان یکسان می‌کنند. بنابراین، ذرات به سرعت سرد می‌شوند.

## Slide 40: Powder Production Techniques
The Hametag (Eddy-Mill) Process and Jet Milling
In this process a ductile material, mainly iron in the form of fine scrap (wires, sheets, etc.) is comminuted by rotating propellers in a vessel under a protective gas. The high speed (up to 85 ms-l ) , generates gas streams in which the particles undergo the main part of their size reduction as self-disintegration. Up to 1950 much of the iron powder used for machine parts production was made by this method. The plate-like particles (0.05 to 0.5 mm) with a relatively smooth surface have only a moderate compressibility and the process has a low efficiency with high energy consumption. This type of mill is no longer in service. New types of jet-mills of different design are widely used, but mainly outside the field of powder metallurgy.
The term 'compressibility' is defined as the ability of a powder to decrease in volume under pressure, and the term 'compactibility' is defined as the ability of the powdered material to be compressed into a tablet of specified strength (i.e. radial tensile strength or deformation hardness).

## Slide 41: Powder Production Techniques
Mechanical Alloying
Mechanical alloying is a high-energy ball milling process for producing composites with a controlled, even distribution of a second phase in a metallic matrix. It was first published in 1970 and introduced in the context of developing dispersion-strengthened alloys (see section 11.9.3), in which strengthening by precipitations and dispersed oxides is combined. The process enables the development of special microstructures essential for achieving good high-temperature mechanical properties in multiphase powder metallurgy materials. In particular, the distribution of a non-metallic phase in a metallic, ductile matrix can be homogenized to a degree, which can be achieved otherwise only by chemical means. Also chemical reactions and formation of solid solutions can be obtained, in such cases the term 'reaction milling' is used. The process consists of long period milling of mixtures, in which the main component (later the matrix) is ductile.

## Slide 42: Powder Production Techniques
As a result of the permanent high energy ball-powder interaction (Fig. 2.8) the ductile phase undergoes a continuous cycle of plastic deformation, fracture and re-welding processes, by which the fine dispersoids are implanted step-by-step into the interior of the ductile phase. This can be understood as a three stage process. In the first stage strong particle deformation ('miniforging') and welding of particles are dominant, while the dispersoid is forced to cover the steadily increased surface of the ductile phase, which embrittles continuously. During the second stage the large lamellar-like particles formed are fractured, forming again new surfaces, which may pick up more of the dispersoid particles, re-weld and form finer lamellae (Fig. 2.9). An equilibrium between deformation and welding on the one hand and fracturing on the other is reached (more or less) during the third stage, while homogenisation proceeds, and the mechanical alloying process terminates.

## Slide 43: Powder Production Techniques
A considerable initial coarsening of the ductile phase can take place, when the starting particle size of the metal powder is very fine (see Fig. 10), while crystallite size decreases. Very effective mechanical alloying has been achieved by attritor milling, but other, more economic, milling processes can also be successful. Longer times, however, have to be allowed with low energy ball mills. Mechanical alloying is applicable to nearly all combinations of brittle phases (oxides, carbides, nitrides, carbon, intermetallics) and ductile metallic powders, which demonstrates the possibilities for extensive composite materials development. The process has also been used for the amorphisation of metal or alloy powders, which is of some interest for the manufacture of metallic glasses. The sintering process, however, has to be carefully adjusted to avoid recrystallization and the temperature of the powders must always be below the glass transition temperature (Tg). Mechanical alloying yields amorphous materials over broader composition ranges than other processes such as splat cooling.

## Slide 44: Powder Production Techniques

## Slide 45: Powder Production Techniques
Processing of Metal Chips
Metal chips produced by cutting or milling during mass production are often treated as scrap, because the handling charges exceed their value as raw material. Nevertheless, attempts have been made by mechanical processing to re-cycle ferrous and non-ferrous chips, from which powders can be produced. This may be economic with expensive non-ferrous metals and alloys such as copper, brass or bronze, when the chips can be delivered with low impurity levels, in sufficient quantities and with uniform quality. The process of powder manufacturing from chips involves first cleaning from impurities. The following fragmentation, which is essential in order to get press and- sinter-grade powders, is done by high energy (e.g. vibration) ball milling. The cold deformed powders have to be annealed in order to improve their compactibility. The process may become more significant in future because of the need to conserve raw materials.

## Slide 46: Powder Production Techniques
Principal Aspects of Atomization
Melt atomization is the most important production method for metal powders. The process generally consists of three stages:
• melting
• atomization (disintegration of the melt into droplets)
• solidification and cooling.
In most cases, additional processing becomes necessary before the powders attain their desired properties, e.g., reduction of surface oxides, degassing, size classification, etc. For each of the process stages different methods can be used, resulting in a large number of variants. Table 2.1 provides an overview of the present situation. The main classification criterion is the way in which the energy for disintegration is introduced into the melt. This can be by capillary forces (melt drop process), mechanical impact (impact disintegration), electrostatic forces (electrodynamic atomization), liquid or gas streams or jets (liquid or gas atomization) , centrifugal forces (centrifugal atomization), gas super-saturation of the melt (vacuum atomization), or ultrasonics (ultrasonic atomization) .

## Slide 47: Powder Production Techniques
In the melting stage the most important criterion is whether melting and melt distribution require a crucible system or not. Crucibles are one of the main sources for contamination of atomized powders. The second criterion is the heating source. Essentially all melting techniques known in metallurgy can be used, e.g., induction, arc, plasma, and electron-beam melting, but some of these may also contribute to contamination, as for example in arc melting.
During the solidification and cooling stage, the cooling rate is the controlling parameter. This depends, of course, on the dimensions of the liquid droplets or solid powder particles, and also on the type of heat transfer from the particles to the surrounding medium. The undercooling prior to nucleation and cooling rate are the controlling factors for determining the microstructure of the powder particles, as well as for the dimensions of the atomization unit, which has to provide a path, on which the droplets can solidify without touching the unit walls or structure. The various melt disintegration methods are explained in more detail below.

## Slide 48: Powder Production Techniques
Methods Based on Capillary Drop Formation
In the melt drop process, the liquid metal flows vertically through the outlet capillary of a tundish, which controls the melt stream diameter, ds. The melt stream breaks up into droplets of a diameter dD, which depends mainly on ds, and only slightly on the melt viscosity, V s, and the surface tension, ys, of the liquid metal. Within the usual range of properties of liquid metals, the correlation between ds and dD can be approximated by equation (2.2).
As the resulting particle size is relatively large and the production capacity quite small, the melt drop process has only been used in laboratory scale production.

## Slide 49: Powder Production Techniques
A smaller particle size can be achieved by impact disintegration of the resulting droplets (Fig. 2.11). The relation between the diameter of the secondary droplets dD2 and dD is given by:
Vp being the impact velocity and Vc the minimum impact velocity at which droplets of the size dD can be broken down. The application potential of this process is for the production of rapidly quenched powders. With a cooled impact surface a cooling rate of more than 107 Ks-1 necessary in the production of amorphous powders is said to be possible.

## Slide 50: Powder Production Techniques
The electrodynamic atomization process has some similarities to the methods mentioned above, because it is also based on droplet formation out of a capillary orifice (Fig. 2.12). A DC voltage of 3-20 kV is applied between this orifice and a perforated electrode plate in front of it. Melt droplets, which have a strong positive charge, are emitted from the orifice. With a capillary diameter of 76 micron, a particle size in the range of 0.1-10 micron has been achieved. This is a very fine powder compared to that from other atomization processes. The production capacity of existing units is only in the order of grams per hour and the process has not yet progressed beyond laboratory scale.

## Slide 51: Powder Production Techniques
Atomization by Liquids
Liquid (generally water) and gas atomization are the most important process variants for industrial powder production. Water atomization is mainly used for the production of iron base powders. Figure 2.13 shows a scheme for a water atomization unit. The starting material is melted and metallurgically treated in a separate furnace and then fed into a tundish. The tundish provides a uniformly flowing vertical melt stream, which is disintegrated into droplets in the focal area of an arrangement of several water jets. Configurations of the water jets may differ in the number of jets, the angle alpha, between the jets and the metal stream, and the focusing of the jets into a point or line. The impact from the high pressure stream of water leads to disintegration of the flowing metal.

## Slide 52: Powder Production Techniques
A high energy input to the water stream is needed. The usual pressure range is 6- 21 MPa, resulting in a velocity of 70-250 m.s-1 of the water jets. Throughput is typically 10-100 kg.min-1 of metal for 0.1-0.4 m3.min-1 water consumed. The overall process efficiency is much better than in the mechanical disintegration of solid materials, but still remains 1%. Atomization occurs under an unsteady state of turbulent flow conditions, which makes a theoretical treatment of the process very complicated. From empirically derived relations it can be concluded, however, that the most important parameters which control the average powder particle size, dD are the water pressure Pw and velocity vw the angle alpha; the melt stream diameter ds, the melt viscosity, melt density, melt surface tension Ys, and the ratio of molten metal to water flow rate (qs/qw). The particle size decreases with increasing component of the jet velocity perpendicular to the melt stream:

## Slide 53: Powder Production Techniques
From the empirically derived equation (2.5) it can be seen that small melt stream diameters, high flow rate ratios (qs/qw), high density, and low viscosity and surface tension of the melt also favour the production of fine particles.
The overall range of the mean particle size attained by water atomization is about 30-1000 micron. Quite different particle shapes can be produced, depending on the process parameters. With decreasing superheating of the melt, increasing jet velocity, and decreasing flow rate ratio the particle shape changes from nearly spherical to irregular. Irregular particle shapes provide a good green strength of the cold compacted powders and are therefore preferred in the production of iron and steel powders for structural part applications.

## Slide 54: Powder Production Techniques
Due to its low capital and operating costs, water atomization is, in terms of output, the most important atomization method. The limiting factor is the reaction of the atomized metal with water. Water atomization is therefore restricted to metals and alloys of low oxygen affinity, which pick up only tolerable amounts of oxygen or which can be reduced easily in a subsequent step. Iron and low alloy steel powders can usually be reduced in hydrogen-containing atmospheres. In some special cases, even iron base powders containing substantial amounts of highly reactive elements are produced by water atomization, e.g., high speed tool steels. In such processes, special measures are necessary, such as adjustment of the carbon content of the melt and vacuum reduction annealing of the powder.

## Slide 55: Powder Production Techniques
The use of high purity liquid steel with low concentrations of interstitial elements ensures the production of powders with highest compressability ('super-compressable powders'), which are used e.g. for low-alloy Mn-Mo-Ni-steels. Their residual oxygen content is, depending on the alloying element, only 0.08-0.15 wt-%.
More recently, synthetic oils have been used as the atomization liquid, thereby reducing the oxidation problem. In oil atomization, however, carbon pick-up occurs in the powders. Decarburization of powders containing reactive elements is, however, less of a problem than is the need for reduction in the case of water atomization. Industrially oil atomization is used for the production of low alloy Mn-Cr steel powders.

## Slide 56: Powder Production Techniques
Gas atomization
Gas atomization is the second most important atomization process. Air, nitrogen, argon or helium are used, depending on the requirements determined by the metal to be atomized. Atomization is undertaken either in vertical or horizontal units. In Fig. 2.14, a vertical unit for inert gas atomization is schematically represented. The process principles are similar to those of water atomization including the problem of mathematical treatment. An empirically derived relation between the process variables and the mean particle size is given in equation (2.6).
A cyclone separator is an economical device for removing particulate solids from a fluid system. The induced centrifugal force is tangentially imparted on the wall of the cyclone cylinder. This force, with the density difference between the fluid and solid, increases the relative settling velocity.

## Slide 57: Powder Production Techniques
where V represents the kinematic viscosity, and G is the index for the atomization gas. Again, a high velocity of the atomizing fluid, small melt stream diameters, high density, and low viscosity and surface tension of the melt favour the production of fine particles. The factor C, is dependent on the geometrical design of the nozzle which forms the gas stream or jets. The nozzle design seems to be an important key to success or failure of a gas atomization system. The overall process efficiency is similar to that of water atomization (i.e. ~ 1%), but the process costs are substantially higher. The throughput of single melt stream installations is up to 50 kg/min. Gas pressures up to 12 MPa are applied, resulting in supersonic gas velocities of up to Mach 2 and a gas flow rate of up to 40 m3. min-1. The gas leaves the atomization chamber through a cyclone, where the fine powder particles are separated before the gas is recycled into the process. Because of the relatively low cooling rates, the atomization chambers are quite large. A complete vertical atomization installation can be up to 20 m in height.
Kinematic viscosity is defined as the ratio of dynamic viscosity to fluid density, expressed in units of m²/s.
Dynamic viscosity is defined as a measure of the resistance to flow in a fluid, characterized for Newtonian fluids by the relationship μ = τ / (dv/dn), where τ represents shear stress, v is the fluid velocity, and dv/dn is the velocity gradient perpendicular to the flow direction.

## Slide 58: Powder Production Techniques
The mean particle size of gas atomized powders is in the range of 20-300 micron. The particle shape is spherical or close to spherical. Irregular particle shapes can only be produced in systems where reactions between the gas and the liquid metal cause the formation of solid surface layers. This is the case, for example, in the air atomization of aluminium.
Melt atomization by air is used in the production of the so-called 'Roheisen- Zunder' (RZ) iron powder. This process starts from a cast iron melt. The surface oxides formed during atomization are reduced by the inherent carbon of the cast iron particles during a simple subsequent annealing treatment.
In aluminum air atomization, a film of oxide is usually formed. The spontaneous oxide formation prevents spheroidization of the individual droplets by surface tension of the liquid metal.

## Slide 59: Powder Production Techniques
A powder low in oxygen and carbon is obtained only when their concentrations within the powder are balanced according to equation (2.7). Since this is normally not the case, a final hydrogen reduction is advisable. As a result of increasing quality demands, the RZ process has now been almost entirely replaced by water atomization. Air atomization is still used in the production of aluminium and aluminium alloys, copper and copper alloys, precious metals, tin and lead powders.
Inert gas atomization is applicable for all metallic alloys which can be melted. The main application is for high alloy products such as stainless steel, tool steels, iron, nickel- or cobalt-base superalloy powders, as well as aluminium alloy powders. Limiting factors are the availability of suitable crucible and auxiliary melting process materials. Powders from refractory metals with high melting temperature and highly reactive materials, such as titanium alloys, are usually produced by other methods.

## Slide 60: Powder Production Techniques
Centrifugal Atomization
The centrifugal atomization processes use centrifugal force for the melt disintegration and involve one or two process steps (Fig. 2.15). In the single step method, a liquid film is produced on the surface of a rapidly rotating consumable alloy bar by an arc (rotating electrode process), plasma, or electron beam source. The electrode or alloy bar, which is rotating at up to 15,000 rpm has to meet stringent requirements as to stability, uniformity and surface quality. The melt cannot be highly superheated, as the molten material then rapidly runs off from the electrode. The two-step process overcomes these problems by the separation of the melting and melt disintegration stages. The latter is performed by a rapidly revolving cooled wheel, disc or cup. The problem with the two-step process is to transfer high rotational velocities to the melt.

## Slide 61: Powder Production Techniques
At low melting rates the melt disintegration occurs by the direct drop formation mechanism DDF (Fig. 2.15). A primary particle is emitted from liquid protuberances at the edge of the rotating disc or cup. This droplet is for a short time linked to the edge by a fine liquid thread, which is also then emitted as a smaller secondary particle. The particle size distribution, therefore, becomes bimodal in the DDF mode. At higher melting rates, the protuberances stretch into ligaments, which break down into strings of many particles by a ligament disintegration mechanism (LD). The proportion of secondary particles increases steadily with the melting rate. At even higher melting rates, a film is formed at the edge of the disc, directly emitting the droplets by a film disintegration mechanism (FD).

## Slide 62: Powder Production Techniques
A mathematical treatment of centrifugal disintegration gives equation (2.8). The liquid droplet diameter decreases with increasing rotational velocity, increasing melt density and decreasing melt velocity.
The particle shape is spherical. One advantage of centrifugal atomization is the narrow range of particle size distribution. The mean particle size, however, is relatively coarse, in the range from 150-250 micron for single step processes. Powders with a mean size of 80-90 micron can only be prepared in two-step installations, where a crucible rotation speed up to 25,000 rpm is feasible.
The main advantage of single step centrifugal atomization is that the melt has no contact with ceramic crucibles or liners. The process is therefore suitable for the production of refractory powders like tungsten, or highly reactive powders, e.g., titanium alloys. The production capacity is low (1-6 kg min-1). Two-step centrifugal atomization is used for the production of aluminium, titanium alloys, superalloys and refractory metal powders.

## Slide 63: Powder Production Techniques
Vacuum Atomization
The vacuum atomization or melt explosion technique utilizes the pressure dependence of gas solubility in metal melts. After vacuum induction melting, the melt is saturated at an enhanced pressure (1-3 MPa) with a gas, usually hydrogen. A ceramic nozzle system is then immersed into the melt to connect it to the evacuated atomization chamber. The gas is spontaneously released and breaks the melt stream down into droplets. The resulting powder morphology is similar to inert gas atomized powders in both particle shape and size distribution.
Vacuum induction melting (VIM) utilizes electric currents to melt metal within a vacuum.

## Slide 64: Powder Production Techniques
Solidification and Cooling
Depending on the different mechanisms of heat transfer (see Table 2.1), the processes described above lead to different cooling rates. The cooling rate itself determines the powder particle shape, its microstructure and, in combination with the in-flight speed, the dimensions of the atomization chamber. Figure 2.17 gives an order of magnitude overview of the cooling rates achieved by the different methods. Cooling occurs by heat transfer via radiation and heat flow through the medium which is in contact with the melt. The melt volume, together with the heat flow, determines the cooling rate during solidification. Small melt volumes favour rapid cooling. Atomization under vacuum or reduced pressure conditions results in relatively low cooling rates.

## Slide 65: Powder Production Techniques
The microstructure of the powder particles is determined by nucleation and growth factors. After nucleation has occurred, the relation of the growth rate of the solid from the liquid and the diffusion rate in the liquid determines the microstructure. A large undercooling increases the growth/diffusion ratio and favours uniform crystal structures. Low growth/ diffusion ratios result in dendritic microstructures as a consequence of segregation. For many common alloys the transition from dendritic to cellular microstructure occurs at a cooling rate of the order of 105K/ s. The secondary dendrite arm spacing is a direct measure of the degree of segregation. It decreases with the cooling rate, as already shown in Fig. 2.17. With increasing cooling rate, the particles tend to form microcrystalline structures, combined with other non-equilibrium states such as high defect concentrations or metastable phases, which promote sintering effectively.

## Slide 66: Powder Production Techniques
Even noncrystalline (amorphous) structures can be obtained. Some processes which can achieve such rates are the droplet impact disintegration method, planar flow casting or melt extraction which uses a fine edged spinning wheel. These utilize chill block cooling and belong to the so called rapid solidification methods. They are widely used for steels, copper, magnesium and aluminium alloys. Rapid solidification, in its different forms, is steadily growing in importance.
The dimensions of the atomization chamber are determined by the solidification time and the in-flight velocity of the liquid droplets. Therefore, large units are required for vacuum processes (e.g. centrifugal atomization and vacuum atomization) and for gas atomization with high speed gas streams. This problem can be reduced by deflector plates, which divert and retard the droplet flow.

## Slide 67: Powder Production Techniques
Particle adhesion to the plates can be inhibited by coating or by regenerating liquid films. Small chamber dimensions are suitable for liquid atomization, due to the high cooling rates, and in ultrasonic atomization, where the droplet velocity remains moderate.
Figure 2.18 shows several powders produced by the most common atomization techniques: water, gas and centrifugal atomization. Spherical particles result from the solidifying droplets in gas and centrifugal atomization as a result of surface tension. Water atomized powders can be produced with very irregular particle shapes for high green strength requirements, but particles close to spherical can also be produced if good flowability and tap density are required.

## Slide 68: Powder Production Techniques
CHEMICAL PROCESSES
- Reduction
  Hydrogen reduction
  Hydrochemical reduction
  Carbon reduction
  Reduction by metals
-Carbonyl Processes
- Hydride-Dehydride Processes
- Electrochemical Processes
  Electrolysis of aqueous solutions
  Fused Salt Electrolysis

## Slide 69: Powder Production Techniques
Reduction
Principle aspects
The main chemical processes in powder metallurgy involve the reduction of metal compounds such as oxides, carbonates, nitrates or halogenides with gases (generally hydrogen) or solids (carbon or highly reactive metals). In most cases the metal compounds to be reduced are in the solid state. However, hydrometallurgical processes have been developed also, especially for the reduction of nickel and cobalt solutions by pressurized hydrogen. When the reaction takes place in the solid state or by solid-gas reaction, no subsequent purification is possible. A sufficiently pure raw material has, therefore, to be provided as a feedstock. For kinetic reasons, the compound to be reduced has to have a suitably small particle size, which should not be exceeded, otherwise the controlling diffusion processes may lead to very long reaction times which are not acceptable in practice.

## Slide 70: Powder Production Techniques
The process is controlled by its free energy of reaction which has to be negative. The more stable the compound, the stronger the reduction media have to be. Some basic thermodynamic data are used for reduction process. The free energies of oxidation for some of the reducing agents are included. Since alkali, and especially alkaline earth metals, form very stable oxides, they are very strong reducing agents. Figure 2.19 also shows the extreme reducing capability of Ca, which is needed when H2, C, CO or Na cannot be used.

## Slide 71: Powder Production Techniques

## Slide 72: Powder Production Techniques
Hydrogen reduction
The reduction of oxides or other compounds with hydrogen is generally undertaken well below the melting temperature of the metal. Examples of technical importance are refractory metals such as tungsten and molybdenum, ferrous metals and copper, which form compounds with only moderate stability. Very pure and fine powders can be obtained. The process is often undertaken in tube furnaces, in which the oxide powder is moved in flat crucibles in the opposite direction to the hydrogen stream. The overall reaction equations such as are simple.

## Slide 73: Powder Production Techniques
In reality, several different reaction steps can be involved, depending on the lower oxide compounds that are stable and the degree of Me-O solid solution. Furthermore, the properties of the resulting powder and, consequently, the reproducibility of the product, are strongly dependent upon the reducing conditions. Some general rules can be stated as follows:
• a higher reduction temperature and a longer time provide: larger particle size, lower specific surface, lower residual oxygen content and (possibly) formation of a 'sintered cake'.
• a lower reduction temperature and a shorter time provide: smaller particle size, higher specific surface, higher residual oxygen content and (possibly) pyrophoric powders (see section 5.1).
• a high flow rate of hydrogen with a low dew-point results in a high reduction rate, low residual oxygen content and no, or very little, re-oxidation during the cooling period.
The dew point or dew point temperature of a gas is the temperature at which the water vapor or low-boiling hydrocarbon derivatives contained in the gas is transformed into the liquid state.
یعنی هیدروژنی که رطوبت بسیار کمی دارد.

## Slide 74: Powder Production Techniques
a low flow rate of hydrogen with a high dew-point would produce the opposite results and would therefore be generally impracticable. The danger of re-oxidation of reduced powders at low temperatures is caused by the temperature dependence of the equilibrium according to equation (2.10) moving to the left hand side at low temperatures. This is shown for the W02 - W reduction in Fig. 2.20.
Chemical equilibria are generally defined by the equilibrium constant K in accordance with the law of mass action. K is the ratio of the concentrations of starting materials to those of reactants, given in this case as
چون اکتیویته مواد جامد MeO و Me تقریباً برابر ۱ در نظر گرفته می‌شود، عبارت ثابت تعادل فقط تابع گازهاست.
اگر نسبت ​​ کوچک باشد → گاز احیایی‌تر است → واکنش به سمت راست (تشکیل فلز) پیش می‌رود.
اگر این نسبت زیاد شود → تمایل به تشکیل اکسید افزایش می‌یابد → ممکن است پودر فلز دوباره اکسید شود.
به همین دلیل است که در دماهای پایین (همان‌طور که در جمله‌ی قبلی گفتی)،
K کاهش می‌یابد و تعادل به سمت چپ (= تشکیل MeO) جابه‌جا می‌شود.

## Slide 75: Powder Production Techniques
Hydrochemical reduction
Several metals can be produced in powder form directly from aqueous (or organic) solutions by reduction with (preferably) gaseous hydrogen. This process has been developed by Sherrit Gordon Mines Ltd, Canada, especially for the production of nickel and cobalt powder from sulphidic ores containing (preferably) Cu, Ni, Co, Fe and S.A convenient technique is the separation of a Cu rich and a Ni + Co rich fraction by flotation of the fine ore with a subsequent leaching procedure in autoclaves with NH40H under air pressures of 7-9 bar. Ni, Co (and the residual Cu) form readily soluble ammines (e.g., Ni [NH3]6 S04: nickel hexammine sulphate), Fe forms insoluble Fe(OH)3 and the Sulphur is transformed to sulphates. Most of the other constituents of the ore are insoluble in ammonia and form a solid phase together with Fe(OH)3. However, a few other metals, like Sn and Cd also enter the solution.

## Slide 76: Powder Production Techniques
The clean solution is then treated with gaseous hydrogen under 28-35 bar
pressure at 180-220°C in an autoclave when the following reaction occurs
(ignoring the complex ions):
Low [H+] and high pH2 shift the equilibrium to the right hand side and facilitate metal precipitation. The electrochemical conditions for the process are summarized in Fig. 2.21. Gaseous hydrogen is able to precipitate metals from their ionic solution, when the H2/H+ potential is more negative than Me/Men+, i.e. in the field below the straight lines. There is a small dependence of the H2/H potential on the H2 partial pressure (as seen by the small distance between lines a and b), but a large dependence on pH value. Thus, most of the metals can be precipitated from alkaline solutions and only a few such as Cu and Ag from stronger acidic liquids.

## Slide 77: Powder Production Techniques
A special application of this process is the preparation of composite powders, when a 'seed powder' is dispersed in the liquid, which has to be kept in continuous motion in order to achieve a homogeneous dispersion. Each powder particle acts as a nucleus and is coated by the deposit. Examples are Ni-coated oxide or graphite and Co-coated diamond particles. The uses of composite powders (see section 4.3.) include avoiding segregation of the components; facilitating the even distribution of a dispersant in a matrix (to prevent particle contacts); improving the wettability in melts etc. Composite powders can also be produced by other methods such as chemical vapour deposition (CVD), physical vapour deposition (PVD) , sol/gel processes, etc. Recently, WC-Co composite powders have been produced in form of nanosized (20-40 nm) particles (see section 2.4) by a spray drying process for manufacturing of special hard metals.

## Slide 78: Powder Production Techniques
Carbon reduction
One of the most important powder production processes is the direct reduction of magnetite ores (Fe3O4) by carbon. The final product, sponge iron powder, is one of the starting materials for the mass production of sintered iron and steel parts, and more than 50% of the iron powder used is produced by this process. The ore is ground to particle sizes of less than 0.5 mm and purified by magnetic separation, up to the iron content of about 71.5%. (the theoretical value is 72.5%.) After drying the ore is poured into cylindrical ceramic capsules, together with mixtures of fine coke and lime in concentric layers. The lime is used to extract the sulphur impurities. A number of capsules is arranged on a transportation unit which is moved through a reduction tunnel furnace, heated by natural gas.

## Slide 79: Powder Production Techniques
The furnace is divided into a heating zone, a reduction zone with a maximum temperature of about 1250°C and a cooling zone, with an overall length of about 270 m. The reduction process, starting at 650-700°C, lasts two to three days, works continuously and is fully automated. The reaction product is an iron sponge formed by slight reaction sintering, which is then crushed, classified and subjected to a final treatment to adjust carbon and oxygen contents and to reduce residual stresses.
Most of the powder is milled to particle size distributions suitable for powder metallurgy parts production, whilst some (particle size> 150 micron) is sold for the manufacture of welding electrodes. It is very important to reduce the carbon as well as the oxygen content (and especially the non-metallic oxide inclusions) to levels acceptable for sintered parts.

## Slide 80: Powder Production Techniques
The reduction process occurs, after an early solid state reaction, mainly via the gas phase, although no reducing gas is introduced:
The overall reaction is while the carbon is in equilibrium according to
, which is strongly dependent on temperature. Side reactions, such as the formation of Fe3C, are not important under the processing conditions. The sponge iron powder has some internal porosity, is of irregular shape and has a good compressibility, although the pressed density is influenced by its micro-porosity. This is a residue of the reduction process and is in contrast to the near pore-free microstructure of water atomized particles.

## Slide 81: Powder Production Techniques
Attempts have also been made to reduce milling 'scale‘ for the production of iron powder. Scale is a high temperature oxidation product of iron and steel and has an overall composition close to Fe304• Reduction processing is simple in principle but technically and commercially feasible only when the scale is available in large quantities, i.e. from big milling plants, producing high purity and uniform quality over long periods. This cannot be achieved, when different (unalloyed and alloyed) steels are milled at the same plant, and which contain Mn, Si, Cr, AI, which form oxides in the scale and which cannot be reduced completely by carbon - the resulting iron powder containing uncontrollable amounts of non-metallic inclusions.

## Slide 82: Powder Production Techniques
Carbonyl Processes
Several metals react with carbon monoxide (CO) under certain conditions to form metal carbonyls (Me(CO)x). Fine metallic powders can be obtained by their thermal decomposition. This is especially important with iron carbonyl (Fe(CO)5, boiling point = 102.7°C) and nickel carbonyl (Ni(CO)4, boiling point = 43°C), from which carbonyl iron and carbonyl nickel powders are obtained. Because of the low boiling point of the carbonyls (which are both toxic and flammable) they can be purified easily by distillation. The resulting metal powders are therefore very pure, except for some carbon and oxygen impurities.
For carbonyl iron production, spongy iron, having a large surface area with high surface activity, is required to obtain an adequate reaction rate.

## Slide 83: Powder Production Techniques
Hydride-Dehydride Processes
The hydride route enables very fine and reactive powders to be produced from metals which are capable of forming solid hydrides. The hydrides are obtained by the reaction of metal with molecular hydrogen at elevated temperatures under a suitable partial pressure. Since they are brittle they can be powdered easily and dissociated in vacuum at similar or somewhat higher temperatures than those at which they are formed. For powder metallurgy, the hydrides of Ti, Zr, Hf, Ta, U, Th, Y and perhaps Mg are of interest. Metal powders produced from hydrides are highly active and often pyrophoric, depending on dissociation conditions. Special precautions, such as inert gas absorption on the powder surfaces, are often necessary in order to avoid instantaneous ignition on exposure to air. Compacts of zirconium powder produced from the hydride can be sintered nearly to full density. Tantalum hydride powder is of some importance in obtaining very pure tantalum carbide powder by carburization, using carbon black. The hydride can be economically obtained from Ta scrap or waste materials. The hydride-dehydride process does not involve any purification of the metal phase. On the contrary, an increase of oxygen and nitrogen can be expected in the final metal powder, depending on the quality of hydrogen and the vacuum system used.

## Slide 84: Powder Production Techniques
Electrochemical Processes
Powder production by electrolysis is a reduction process in which the metal ions are neutralized by the cathodic current. The cathodic potential necessary for deposition depends on the position of the metal in the electromotive series and on special inhibiting electrode processes, which can produce a voltage surge necessary for deposition. Whenever possible the process is carried out in aqueous solutions (e.g. for Cu, Fe, Ni, Co, Zn, etc). Highly reactive metals (e.g. Be, Ta, Nb, Th, etc.) which form highly stable oxides, have to be deposited from molten salt electrolytes. While aqueous solutions are employed at slightly elevated temperatures (up to 60°C) the molten salt process needs higher temperatures, depending on the melting point of suitable (binary or ternary) salt eutectics which should contain a reasonable concentration of the metal to be deposited. The powder can be obtained directly or indirectly, the latter by milling of the often hydrogen-embrittled deposits. The main process parameters to be considered are: metal ion concentration, electrolyte conductivity, temperature, voltage, current density and bath circulation, and, in special cases, the addition of colloids in order to inhibit the growth of nuclei. In aqueous solutions, low temperature and high current density facilitate the precipitation of powder rather than larger deposits.

## Slide 85: Powder Production Techniques
CERAMIC POWDERS
Since the boundaries between powder metallurgy and ceramics are no longer strictly defined, some information on ceramic powders is useful in the context of powder metallurgy. This applies mainly to advanced ceramics. While for the traditional silicate ceramics in general use are natural raw materials (clay, kaolin, etc.), the processing of advanced ceramics requires pure and well-defined powders normally made synthetically. Also the manufacture of ceramic parts is to some extent similar to powder metal1urgy processing. It is convenient to subdivide this field into oxide and non-oxide ceramics. The synthesis of ceramic powders employs a wide variety of methods, yielding powders of very different particle size distribution and specific surface, chemical and phase composition, purity, compactibility, sinterability, etc. Sinter grade powders for manufacturing dense, fine-grained parts must be produced in the lower micron or even sub-micron range with specific surfaces between 5 and 15 m2g-1or higher. Applications of coarser powders (Al203, SiC) include abrasives, refractories (Al203, Zr02, MuIlite), etc.
The principle methods for production are as follows:

## Slide 86: Powder Production Techniques
Solid state reactions: Hydroxides, carbonates, sulphates, oxalates and other compounds can be thermally decomposed to oxides by well known chemical reactions. Depending on temperature-time, loose or agglomerated powders or a sintered cake result, which have to be milled to the desired particle size. In principle the majority of the oxide powders can be produced by this method. The precursor compounds are obtained by either liquid or gas processes. Carbides are made by reaction of metals or oxides with carbon. One of the most important industrial processes is the Acheson method for the production of a SiC from SiO2 (see section 2.3.4), in which it is possible that part of the reaction occurs via the gas phase.
این فرآیند بر اساس کربوترمی (واکنش در حضور کربن در دمای بالا) استوار است و در یک کوره مقاوم الکتریکی به نام کوره اَچِسون انجام می‌گیرد.
مواد اولیه: مخلوطی از سیلیس (ماسه کوارتز، 2SiO​) و کک نفتی (کربن خالص،) با درصد استوکیومتری تقریبی به دست می‌آید.
ساختار کوره: مواد اولیه در اطراف یک هسته مرکزی گرافیتی قرار داده می‌شوند که به عنوان الکترود مقاومتی عمل می‌کند.
حرارت‌دهی: جریان الکتریکی بسیار قوی از طریق الکترود مرکزی عبور داده می‌شود. این امر باعث می‌شود که دمای کوره به شدت بالا برود و به حدود ۲۵۰۰ درجه سانتی‌گراد برسد.
واکنش: در این دمای بالا، کربن با دی‌اکسید سیلیکون واکنش داده و کاربید سیلیکون تولید می‌کند و آب به عنوان محصول جانبی خارج می‌شود:
SiO2(s)+3C (s)→High Temp SiC (s)+2CO (g)
نتیجه: پس از سرد شدن، محصول نهایی در اطراف هسته الکترود مرکزی، توده‌ای از کریستال‌های کاربید سیلیکون را تشکیل می‌دهد.

## Slide 87: Powder Production Techniques
Solid-gas reactions. Oxides, carbides and nitrides may be synthesised by the reaction of metals with oxygen, hydrocarbons, nitrogen or ammonia respectively. While this is less important for oxides, it is a technique used, for example, for the synthesis of ~ SiC and Si3N4, the latter sometimes under increased N2 pressure.
• Gas-phase reaction. Vapour phase decomposition or hydrolysis in a flame is a common technique for the production of TiO2 and SiO2 from halogenides TiCl4 and SiCl4, according to the reaction (for Si02):
(2.34)
High purity powders with extremely high specific surface areas (100 m2g-1 and higher) with only very little agglomeration of the powder particles, are obtained in this continuous process.
Melting processes. Oxides such as Al2O3 and ZrO2 are manufactured on a large scale by arc-melting with subsequent milling to make powders of different particle size ranges. The process is mainly used to produce coarse grade powders for the manufacture of refractories.

## Slide 88: Powder Production Techniques
POWDERS FROM SOLUTIONS
In several techniques an aqueous or non-aqueous solution of salts is the precursor for preparing powders. After solvent removal, the solid residue is thermally converted to ceramic or in some cases metallic powders. The solutions are normally homogeneous on an atomic scale, but the degree of homogeneity of the residue, however, depends on the solvent removal technique. Extremely fine powders, powder mixtures and powders with uniformly distributed additives (e.g., to improve sintering), are obtainable.
This field may be subdivided as follows:
Precipitation and filtration of single compounds or mixtures.
Hydrothermal reactions
Solution combustion.
Solvent vaporization or dehydration

## Slide 89: Powder Production Techniques
The Sol-gel Process
In a separate sub-group are gelation-dehydration techniques in which liquid droplets are transformed into a gelatinous state from which the powder is obtained. These sol-gel techniques now play an increasing role in the preparation of advanced ceramics. The techniques consist in the formation of a three dimensional network of inorganic matter (gel) from colloidal or molecular solutions of the precursor (sol). This reaction takes place in aqueous or nonaqueous media, e.g. by diminishing the water content, by changing the PH-value or the surface charge (zeta potential) of the sol, or by other means which can lead to gelation of the liquid precursor. A wide variety of methods may be used, producing small uniform spheres or powders. The process was developed in the early 1960s for the preparation of micro-spheres of oxide nuclear fuels, consisting of highly reactive agglomerates of very fine particles, which can be sintered at low temperatures to very high densities.

## Slide 90: Powder Production Techniques
ULTRAFINE POWDERS (NANOCRYSTALS)
Although the terms in the finest particle size range are not clearly defined it may be distinguished as follows: submicron particles are per definition below 1 micron, preferably down to 0.5 micron, ultrafine particles between 0.5 micron and 0.1 micron (100 nm) and nano-sized (nano-crystalline) powders less than 100 nm, many of them range between 50 and 20 nm. Such powders have become of increasing interest in the last years for both scientific and technical reasons.
Their processing, and sintering behaviour is unique due to their high surface to volume ratio. Several methods have been used in the past in order to obtain ultrafine powders, such as:
Gas phase reactions in a DC, RF or microwave plasma, Gas phase reaction powered by a laser, Hydrogen reduction of metal chloride vapours, Evaporation and condensation techniques, Processing of solutions.

## Slide 91: Powder Production Techniques
WHISKERS AND SHORT FIBRES
Whiskers are short metallic or non-metallic, usually monocrystalline fibres, which are deposited generally by a vapour-phase process. Whiskers of metallic elements such as Ag and Cu and also of several compounds have been known for a very long time as naturally grown minerals. Scientific and technical studies of whiskers began in the 1940s. The condition for whisker formation (instead of 'normal‘ crystals or crystallites) is a strongly anisotropic unidirectional growth, which often appears under undisturbed growth condition within a certain concentration and temperature range. Whiskers can be easily obtained from most metals and several ceramic materials (such as Al203 and SiC). Some are manufactured industrially in greater than experimental quantities although there is considerable concern about the safety of handling whiskers which has held back keen exploitation. For most whisker manufacturing processes volatile compounds are needed from which the deposition occurs on solid or liquid substrates. Metallic whiskers can be obtained by the reduction of a metal halogenide vapour with hydrogen in a carrier gas at normal reduction conditions.

## Slide 92: Powder Production Techniques
Whiskers can be obtained in a wide range of diameters (from 0.1 to several micron) and lengths (10 to several hundred micron; in some cases up to several millimetres), depending on the material and the processing conditions. The length/diameter ratio ('aspect' ratio) ranges from 20 to several hundred and is an important figure. The cross section of whiskers can be hexagonal, rectangular or even irregular, depending upon crystal structure and growth conditions. Hollow whiskers, stacking faults, kinks and impurities are frequent and determine the quality of the material and its efficiency for reinforcement purposes. The most outstanding property of whiskers is their extremely high strength, which is strongly dependent on diameter and length: the smaller the diameter, the greater the strength. The reason for this is that a smaller section will have fewer or no glide dislocations. This is important for the strength of metallic whiskers, while in ceramic whiskers minimizing of the flaw size, including surface flaws, is the decisive feature.
Surface energy, E = elastic modulus, a = atomic distance

## Slide 93: Powder Properties and Characteristics
The common powder metallurgy terminology for the description of these elements is given in Fig. 3.1. The term powder particle always stands for the primary particles, which do not develop by agglomeration of other particles, but are directly formed as individual particles during the production process. These powder particles can be amorphous or crystalline. Crystalline particles are either single crystals or consist of several crystals or grains (polycrystalline). Polycrystalline powders can be single- or multi-phased. The powder particles can form secondary particles or agglomerates, as shown in Fig. 3.1. In the powder metallurgy process, agglomeration often occurs unintentionally, but can also be intentionally produced by controlled stages. Agglomerates are defined as solid particles which are composed of other particles. This definition is independent of the nature of the attractive forces which cause the primary particles to form the agglomerate. Sometimes the term agglomerate is restricted to weak bonding between the primary particles. Hard agglomerates with strong bonding are then called aggregates.

## Slide 94: Powder Properties and Characteristics
3.2 PARTICLE SIZE DISTRIBUTION
3.2.1 PRINCIPAL ASPECTS
For a number of equally sized spheres or cubes the particle size characteristics are simply given by one measurement. The individual particles of practical powders usually differ in shape and dimensions. The particle shape can deviate significantly from the ideal geometries mentioned above. The size characteristics of powders have therefore to be treated under two aspects: first, the real meaning of the determined size parameter, secondly the statistical distribution of this parameter, which has to represent the total number of particles in the powder. The size parameter is identical with a real linear dimension of the particles only in some exceptional cases. Most methods for particle size measurement yield a size-dependent property of the particle. This property is then related to a linear dimension. The sieve diameter, for example, is the length of the minimum square aperture through which a particle will pass. The particle could be a sphere with the diameter of this aperture, or an elongated platelet with only one axis corresponding to the sieve diameter, a second axis much larger, and the third axis possibly smaller than the sieve diameter.

## Slide 95: Powder Properties and Characteristics

## Slide 96: Powder Properties and Characteristics
In order to calculate the statistical distribution of the size parameter, it is necessary to characterize a statistically representative sample of the powder. The size characteristics can then be presented as distribution functions. These distribution functions represent the quantity proportion of particle belonging to a given size parameter Zi. Quantity proportions are formulated either as cumulative distribution Q(Zi), or frequency distribution q(Zi) (Fig. 3.3). Q(zi) gives the normalized quantity proportion of particles smaller than a size parameter Zi. The frequency distribution q(Zi) is defined as the fraction within a size class, divided by the class width.

## Slide 97: Powder Properties and Characteristics

## Slide 98: Powder Properties and Characteristics
METHODS OF PARTICLE SIZE ANALYSIS
These methods can be classified into: counting methods, sedimentation methods, separation (classification) methods, and light scattering and diffraction methods. The counting methods can be subdivided into direct and indirect methods, depending on whether the particles themselves are measured, or particle images or projections. Microscopy, for example, is an indirect counting method. With direct methods, the particles directly trigger the measurement. The Coulter principle (see section 3.2.4.5) is such a method. Sedimentation methods utilize the free-falling velocity of particles in a gravity or centrifugal field. Separation of the particles into different size classes and measurement of the fractions of every size class is realized in classical sieve analysis and in the fluid classification methods. The light scattering and diffraction methods analyze diffraction patterns of particles. Diffraction methods have become increasingly important in powder metallurgy and ceramics in recent years because of their versatility regarding measurable size range, and high speed of operation.
The instrument, the Coulter counter, measures the number of particles above a preset particle volume which are present in a suspension. One can determine the particle-size distribution from the counts at different preset threshold volumes and the total particle number per unit volume of the suspension.

## Slide 99: Powder Properties and Characteristics
Sieve Analysis
Sieving is an obvious method of powder classification and one of the simplest and most widely used in particle size analysis. Sieves are characterized by their aperture size in micron or mm, and are often also referred to by their mesh number, which is the number of wires per linear inch. A high mesh number thus implies a small aperture, for example 400 mesh corresponds to a 37 micron aperture with a wire thickness of 26.5 micron. The sieves are made of either woven wire, punched or electroformed plates. The apertures of woven wire sieves are considered to be squares, although they deviate somewhat from this shape, due to the three-dimensional structure of the weave. Electroformed micromesh sieves are available with round and square apertures. Dry sieving is applicable to relatively coarse non-cohesive powders, fine and cohesive powders have to be analysed by wet sieving. The sieving operation is either performed by hand, or by various types of sieving machines. In machine sieving, the normal practice is to use a stack of sieves with an ascending order of aperture sizes, placing the powder on the top sieve. The sieves are subjected to simple vibration or more complicated patterns of movement.

## Slide 100: Powder Properties and Characteristics
Microscopy
Microscopy is one of the counting methods, in which each individual particle is observed and measured. In addition to particle size, microscopy can also give other information such as the particle shape and the state of agglomeration. The problem in the use of microscopy is the representativeness of the sample, as microscopical measurements are carried out on very small sample quantities and the sampling method can cause agglomeration. Optical as well as electron microscopy are employed for particle size measurement. Optical microscopes can be used for particles down to about 0.8 micron In this range of sizes the particle dimensions reach the wavelength of light which causes scattering and diffraction. The reflection mode is applicable down to 5 micron; for particles less than 5 micron the transmission mode has to be used. Electron microscopy enables the measurement of particles down to the nm range. Sub-micrometre particles are often transparent to high voltage electrons, which enables additional information on the crystalline structure and structural defects of the particles. Clearly this approach is extremely time-consuming if statistically significant information is to be obtained. Generally it is employed to gather an idea about the size distribution and the variation in particle size.
وقتی نمونه بسیار نازک باشد (که ذرات زیر میکرومتری آماده شده برای TEM اغلب نازک هستند)، بیشتر الکترون‌های پرانرژی می‌توانند بدون برهم‌کنش شدید از نمونه عبور کنند. این خاصیت به عنوان “شفافیت” شناخته می‌شود. استفاده از “ولتاژ بالا” (مثلاً ۳۰۰ کیلوولت یا بیشتر) باعث افزایش قدرت نفوذ الکترون‌ها می‌شود.

## Slide 101: Powder Properties and Characteristics
Scanning electron microscopy (SEM) utilizes medium energy electrons (5- 50keV) in a fine « 0.01 micron) beam scanning the observation area. Secondary (SE) and backscattering electrons (BE) are counted by suitable detectors. Secondary electrons arise from the near surface regions of the particles and give high resolution images. Backscattered electrons arise from the somewhat larger volume of the particles near the electron beam, causing a slight reduction in resolution. They are dependent upon the atomic number of the element emitting them, resulting in a material contrast for regions of different atomic composition. This makes it possible to distinguish between different compositions in powder mixtures as long as there is a sufficiently large difference in atomic number between the elements. Also wavelength and energy disperse X-ray techniques can give more quantitative compositional information. Sample preparation is a difficult problem in all microscopical methods. Each particle to be measured has to be isolated from the neighbouring particles. Most preparation techniques therefore use suspensions with low concentrations of the particles. These suspensions are applied to the microscope slide, electron microscope grid, or target stub and allowed to evaporate. There are various methods used for the fixing of the particles. TEM and SEM samples are coated with thin carbon or metal films to prevent charging effects. In many cases, analyses have to be made from the projected images of the particles. This of course ignores internal porosity and concave parts of the surface. A more precise technique is therefore to examine sections from a random sectioning of the particles. This can be done for particles > 10 micron by the normal metallographic grinding and polishing methods.

## Slide 102: Powder Properties and Characteristics
Diameters commonly used are (see Fig. 3.8):
• Feret's diameter, the distance between two tangents on opposite sides of the particle. This is a one-dimensional projection of the perimeter of the particle outline.
• Longest dimension, the maximum value of Feret's diameter.
• Maximum chord, the maximum length of a line parallel to some fixed direction and limited by the contour of the particle.
• Perimeter diameter, the diameter of a circle with the same circumference as the particle perimeter.
• Projected area diameter, the diameter of a circle with the same area as the described projection.
• Diameters of inscribed or escribed circles.
A number of definitions exist for the particle shape factor Ψ,e.g.:
Ψ = Perimeter / (4ᴫ. projected area), or
Ψ = max. Feret's diameter/ (Feret's diameter in a perpendicular direction)

## Slide 103: Powder Properties and Characteristics
Surface roughness is another particle characteristic. Particles of the same size and shape but different roughness can be distinguished by their fractal dimension, D (see Fig. 3.8). The fractal dimension accounts for the fact that the estimated parameter P, tends to increase, as the step size l at which surface details are resolved increases. P, is given by
If the perimeter is measured by a polygonal line arrangement with varying step length I, and log Pl is plotted against l, the results form a straight line with the slope 1-D. The steeper the line, the more rugged the outline of a particle. An ideally smooth surface has a fractal dimension equal to unity, i.e. it gives a horizontal line.
بُعد فراکتالی معیاری است که نشان می‌دهد یک شیء چقدر فضا را در ابعاد مختلف “پر” می‌کند. این بُعد معمولاً یک عدد غیرصحیح و کسری است.

## Slide 104: Powder Properties and Characteristics
جریان آرام یا laminar
Re​<0.1 (یا گاهی تا ۱)
در این ناحیه، نیروهای ویسکوز غالب هستند.
قانون استوکس (Stokes’ Law) برای محاسبه Fd​ (Fd= 3ᴫμDv ​) معتبر است.
این ناحیه برای اندازه‌گیری ریزترین ذرات در محیط آزمایشگاهی ایده‌آل است.
عدد رینولدز (Reynolds Number)، که با Re نشان داده می‌شود، یک پارامتر بدون بُعد (بدون واحد) بسیار مهم در مکانیک سیالات است. این عدد نسبت نیروهای لختی (اینرسی) به نیروهای ویسکوز (الزجه) در یک سیال در حال جریان است.
به طور خلاصه، عدد رینولدز معیاری برای پیش‌بینی الگوی جریان سیال (آشفتگی یا آرامش آن) است.

## Slide 105: Powder Properties and Characteristics
Light Scattering and Diffraction Methods
Sizing methods which make use of the interaction of electromagnetic waves with the particles have already been mentioned in connection with x-ray and photo sedimentation. These methods apply radiation scattering not directly for sizing but for the estimation of the particle concentration in a suspension. However, scattered radiation also gives information on the size characteristics and can therefore be used in direct sizing methods. Although this has been known for a long time, the practical applications of such methods, mainly based on optical radiation, has only become common during the last decade. Three modern technologies, lasers, optic fibers and computers, have made this development possible. The principles of these methods are based on the interaction of an incident optical beam with a single particle. This beam can either be absorbed, scattered, or transmitted. Scattering includes reflection, refraction and diffraction. The scattering intensity, I, in the distant field (r» D) is of the general form:

## Slide 106: Powder Properties and Characteristics
زاویه تتا (θ)
θ زاویه‌ای است میان جهت تابش اولیه و جهت مشاهده‌ی پراکندگی
یعنی زاویه پراکندگی یا Scattering Angle
وقتی θ = 0 → پراکندگی به جلو (Forward scattering)
وقتی θ = 180° → پراکندگی به عقب (Backward scattering)
زاویه فی (φ)
φ زاویه‌ای است که صفحه‌ی پراکندگی را تعیین می‌کند
در واقع زاویه‌ای است در صفحه‌ی عمود بر جهت تابش (محور z)
از دید هندسی یعنی چرخش حول محور تابش
اهمیت فیزیکی:
در بیشتر حالت‌ها (وقتی ذرات کروی باشند و تابش قطبیده نباشد)، شدت پراکندگی به φ وابستگی ندارد
اما اگر:
نور ورودی قطبیده باشد، یا
ذره شکل غیرکروی داشته باشد،
آنگاه شدت ممکن است با φ هم تغییر کند.

## Slide 107: Powder Properties and Characteristics
شدت سیگنال پراکندگی: هر ذره‌ای که از “Illuminated Sensing Zone” عبور می‌کند، یک “پالس” از نور پراکنده شده تولید می‌کند که به آشکارساز می‌رسد.
دامنه (Height) این پالس مستقیماً متناسب با شدت نور پراکنده شده است.
قانون پراکندگی مای (Mie): می‌دانیم که شدت نور پراکنده شده به اندازه (D) و جنس (m) ذره بستگی دارد.
ارتباط با اندازه ذره: در بسیاری از روش‌ها، رابطه مستقیمی بین Impulse Height (دامنه پالس) و قطر (D) ذره وجود دارد. ذرات بزرگتر معمولاً پالس‌های با ارتفاع (دامنه) بیشتری تولید می‌کنند (البته این رابطه پیچیده است و به زاویه پراکندگی هم بستگی دارد).

## Slide 108: Powder Properties and Characteristics

## Slide 109: Powder Properties and Characteristics
aspect factor, k, depends upon the size and shape distribution of
the powder
flow rate V'.

## Slide 110: Powder Properties and Characteristics

## Slide 111: Powder Properties and Characteristics

## Slide 112: Powder Properties and Characteristics

## Slide 113: Powder Properties and Characteristics

## Slide 114: Powder Properties and Characteristics

## Slide 115: Powder Properties and Characteristics

## Slide 116: Powder Properties and Characteristics

## Slide 117: Powder Properties and Characteristics
هر پودری که در یک ظرف ریخته می‌شود، پس از تکان دادن یا لرزش (تپینگ)، در نهایت به یک چگالی ماکزیمم (یا حدی) می‌رسد که در آن، دیگر ذرات فضای کمتری برای حرکت و قرارگیری بهینه‌تر پیدا نمی‌کنند. این حالت نشان‌دهنده حداکثر فشردگی ممکن تحت شرایط ارتعاش مشخص است.
شرط رسیدن: این چگالی حدی تنها زمانی قابل دستیابی است که همه ذرات در یک “موقعیت ایده‌آل” (ideal position) قرار گیرند. منظور از “موقعیت ایده‌آل”، آرایشی است که در آن فضاهای خالی (Pores) بین ذرات به حداقل ممکن رسیده باشد، یعنی بیشترین تعداد ذرات ممکن در کمترین حجم ممکن جای گرفته باشند.

## Slide 118: Powder Properties and Characteristics
ذرات فولاد به دلیل سختی و الاستیسیته بالاتر، هنگام برخورد با ذرات دیگر یا بستر، انرژی جنبشی خود را عمدتاً به صورت ارتعاش برمی‌گردانند تا تغییر شکل دائمی (پلاستیک) یا تولید گرمای شدید. این خاصیت باعث می‌شود که ذرات در اثر ضربه “جهش” کرده و در فضاهای خالی بهینه‌تر مستقر شوند، در حالی که ذرات سربی (که نرم‌تر هستند) انرژی ضربه را بیشتر به صورت تغییر شکل پلاستیک (له شدن یا چسبیدن) جذب کرده و در نتیجه در آرایش‌های کمتر متراکم گیر می‌کنند.

## Slide 119: Compaction and Shaping
مفهوم محیط حامل با نقطه ذوب پایین
این تکنیک، که اغلب در فرآیندهایی مانند قالب‌گیری تزریقی پودر (Powder Injection Moulding - PIM) استفاده می‌شود، شامل ترکیب پودر مورد نظر (مانند فلزات، سرامیک‌ها) با یک ماده “حامل” است که:
نقطه ذوب پایین دارد: این ماده حامل معمولاً یک پلیمر یا موم است که در دمای نسبتاً پایین ذوب می‌شود.
عملکرد: این محیط حامل به عنوان یک “روان‌کننده” و “چسب” عمل می‌کند و به پودر اجازه می‌دهد تا به صورت یک مخلوط همگن (Slurry یا Feedstock) درآید. این کار ویسکوزیته مخلوط را برای عملیاتی مانند تزریق (Injection) تنظیم می‌کند.

## Slide 120: Compaction and Shaping
پل‌بندی چیست؟ این پدیده زمانی رخ می‌دهد که ذرات پودر (به ویژه ذرات با اندازه‌های متوسط یا درشت) هنگام ریختن در یک ظرف، به جای نشستن در حفره‌های کوچک موجود، بر روی یکدیگر در فضاهای بزرگتر قرار گرفته و مانند دهانه یک پل، یک ساختار قفسی موقت ایجاد می‌کنند.
نتیجه: این ساختارهای پل‌بندی شده، فضاهای خالی (Voids) زیادی را در توده پودر به دام می‌اندازند و اجازه نمی‌دهند که ذرات به طور کامل در کنار یکدیگر فشرده شوند، در نتیجه چگالی ظاهری (Bulk Density) به شدت کاهش می‌یابد.

## Slide 121: Compaction and Shaping

## Slide 122: Compaction and Shaping

## Slide 123: Compaction and Shaping

## Slide 124: Compaction and Shaping